Aspects of the Development of a New Copper Electrowinning Cell based on Reactive Electrodialysis

L. Cifuentes1, R. Glasner1, G. Crisóstomo1,

J. M. Casas2 and J. Simpson3

1 Depto. Ingeniería de Minas, Universidad de Chile, Tupper 2069, Santiago, Chile

2 Depto. Ingeniería Química, Universidad de Chile, Beauchef  861, Santiago, Chile

3 Depto. Ingeniería Metalúrgica, Universidad de Santiago, Av. B. O'Higgins 3363, Santiago, Chile

201St Meeting Electrochemical Society

Philadelphia

May 2002

Limitations of conventional copper electrowinning cells

- low mass transfer rates due to low electrolyte flowrates, which limit the cell current density;

- low specific cathode surface area (m2/kg), which also limits the copper deposition rate;

- high energy requirements (about 2kWh per kg of deposited copper) caused by anodic reaction

(2 H2O  O2 + 4 H+  + 4 e)

with high equilibrium potential and high anodic overpotential, resulting in a 2 V cell  voltage;

- anodic reaction which produces acid mist, causing environmental problems.

Objective

This work aims to contribute to the development of a copper EW cell which simultaneously overcomes the main limitations of conventional technology.

Ways to overcome EW cell limitations:

- new cell designs to allow for electrolyte agitation;

- mesh or particulate cathodes to increase the specific cathode surface area;

- alternative anodic reactions, with less positive equilibrium potentials, lower anodic overpotentials and which do not produce acid mist;

- alternative anodic materials to decrease the anodic overpotential.

Proposals

- Kammel, 1982, has considered 12 alternative cell designs and concluded that the most promising ones are the particulate bed cell and the fluidized bed cell.

- 'Moving bed' or 'circulating bed' cells have been developed

- The sustitution of an alternative anodic reaction has been studied. The one which has shown more promise is the ferrous to ferric ion oxidation

(Fe2+  Fe3+ + e).

- Various anode materials which have a catalytic effect on the ferrous/ferric reaction have been studied

- One way of using the ferrous/ferric anodic reaction while  avoiding a decrease in cathode current efficiency due to ferric ion reduction, is to separate the anolyte from the catholyte (e.g. in a reactive electrodialysis (RED) cell).

RED cell

In a reactive electrodialysis cell, anolyte and catholyte are separated by an anion membrane which hinders cation transport between compartments.

Results

The present work used a copper mesh cathode and various anode materials in an RED cell.

Catholyte : cupric sulfate in sulfuric acid

Anolyte :  ferrous sulfate in sulfuric acid

(various concentrations)

An anion membrane separated catholyte from anolyte.

Both anolyte and catholyte were recirculated by means of peristaltic pumps.

- The electrochemical kinetics of the ferrous/ferric reaction was characterized on : lead sheet, platinum sheet, graphite rod, Pt (as a surface layer on Ti mesh), RuO2 (on Ti) and IrO2 (on Ti) by means of potentiodynamic sweeps.

iL = limiting c.d. of the anodic reaction

Estart =  starting potential for O2 evolution

Table 1	Kinetics of the Fe2+ /Fe3+ reaction

Material		iL, A/m2		Estart, V

Pt			290 			1.8

RuO2/Ti		260			1.7

IrO2/Ti		330			1.7

Graphite		290			1.5

Lead			<10			1.7

The ferrous/ferric reaction on Pb exhibits a very low exchange current density even at high overpotentials, therefore, Pb is not a suitable anodic material for this reaction.

- In the RED cell which uses the ferrous/ferric reaction and catalytic anodes, the graphite anode affords a degree of electrocatalysis which is similar to that of more expensive materials.

- The cell voltage for the Fe2+/Fe3+ reaction was measured for various anode materials at constant cell current density. Results are in Table 2 and show that the cell voltage is lower by 30-60% than those obtained in conventional copper EW cells. The anodic materials, in decreasing order of performance, are: Pt > Pt/Ti > RuO2/Ti  IrO2/Ti  graphite.

Table 2 		Cell voltages RED cell (V)

icell, A/m2		200	250	400

Material

Pt			0.97	1.23	1.72

Pt/Ti			1.07	1.29	1.88

RuO2/Ti		1.17	1.35	1.92

IrO2/Ti		1.18	1.38	2.02

Graphite		1.19	1.40	2.04

- The cell voltage can be further reduced by optimizing (decreasing) the thickness of the anolyte and catholyte compartments

- The separation of Fe and Cu species in the RED cell is achieved by means of anion membranes. Cu ions are retained in the catholyte, where they are electro-deposited on copper sheet or copper mesh cathodes. Results for cell voltage depending on membrane type ('low' and 'high' selectivity) and number are shown in Table 3, where A = anolyte and C = catholyte.

# Table 3		Anion membrane performance

(4 hour runs)

# System			Vcell			Cu (A) 	Fe (C)

V				ppm		ppm

1 low sel.		1.23	         	4.8           	5.1

# 2 low sel.		1.38	         	1.2         	0.4

# 1 high sel.      	1.17	         	1.8          	0.9

# 2 high. sel.     	1.30	         	0.9          	0.3

# Conclusions

Copper electrowinning was carried out in a

reactive electrodialysis cell

Copper mesh cathodes were used

Ferrous/ferric ion oxidation was used as anodic reaction

Lead is unsuitable as an anode material to carry out the electrolytic ferrous/ferric oxidation

Pt, RuO2-Ti, IrO2-Ti and graphite were suitable as anode materials and exhibited similar behaviour

Cell voltages ranged between 0.97 and 1.72 V for the most catalytic material (Pt) at c.d.'s between 200 and 400 A/m2

Cell voltages ranged between 1.19 and 2.04 V for the least expensive material (graphite) at c.d.'s between 200 and 400 A/m2

Best separation results for cation transfer between

anolyte and catholyte were achieved with two

high selectivity anion membranes