# BIOLEACHING OF COPPER SULFIDES

# T. Vargas

Centro de Hidrometalurgia/Electrometalurgia

Universidad de Chile

Facultad de Ciencias Físicas y Matemáticas

tvargas@ing.uchile.cl

INTRODUCTION

The hydrometallurgical treatment of copper sulfide ores or concentrates involves a stage of leaching, in which the copper contained in the copper sulfides is dissolved into a solution.  The copper contained in this solution, the leaching solution, can then be recovered via solvent extraction and electrowinning, producing copper cathodes with 99.99 % copper which can be directly comercialized.

To leach a copper sulfide it is necessary to remove electrons from the sulfide, process which helps to break the sulfide structure and release the contained copper.  This process corresponds to the anodic dissolution of the sulfide and can be represented,  for for the cases of covellite and chalcopyrite, according to the following electrochemical reactions:

CuS           Cu+2 + S0 + +2e							      (1.1)

CuFeS2    Cu+2 + Fe+2  + S0 + 4e							      (1.2)

In leaching operations removal of electrons from the sulfides is achieved by introducing in the leaching solution an oxidative agent. In thermodynamical terms, this oxidative agent can be any redox pair with a thermodynamic potential more positive than the one associated to the anodic dissolution of the respective copper sulfide. Then the thermodynamic driving force for the dissolution of a sulfide is the potencial difference between the semireaction associated to the sulfide and the oxidant, E,   which triggers the transfer of electrons from the sulfide to the oxidant. This process is schematically represented in the scale of standard potentials in Figure 1.1 for the case of leaching of covellite with ferric ion.  Electrons flow naturally from the more electronegative reaction, which occurs to the left, to the more electropositive  semireaction, which occurs to the right. The  number of electrons released and accepted needs to be equal, thus the global reactions is obtained as follows:

CuS  Cu+2 + S0 + 2e								        (1.3)

2Fe+3 + 2e  2Fe+2									        (1.4)

CuS + 2Fe+3  Cu+2 + 2Fe+2 + S0							        (1.5)

E0, V(SHE)

+ 0.77

+ 0.55

Fe+3 + e-   Fe+2

Cu+2 + S0 + 2e-  CuS

e-

Figure 1.1. - Flow of electrons in semi-reactions involved in the ferric leaching of covellite

The potential associated to each of the semireactions involved in the leaching of covellite can be calculated using to the Nernst equation. Thus for semi-reaction 3:

ECu+2CuS=+0.55+RT2FlnCu+2					            (1.6)

And for  semi-reaction 4:

EFe+3Fe+2=+0.77+RTFlnFe+3Fe+2

(1.7)

As the leaching reaction proceeds the Fe+3/Fe+2 ratio in solution decays and EFe+3/Fe+2 shifts towards more  cathodic potentials. On the other hand, Cu+2 decreases and ECu+2/CuS shifts towards more anodic potential. Consequently the  driving force for the sulfide dissolution, E, decays with leaching time. For the leaching process to be mainatined efficiently it is necessar to keep the thermodynamic driving force its maximum. Therefore,  it is necessary: a) to continuously remove cupric ions from solution. This is normally achived in practice by selective extraction of cupric ions in a solvent extraction operation; b) to continuously regenerate ferric ion from ferrous ion oxidation. In bacterial leaching this aim is achieved by catalyzing the reoxidation of ferrous iron with oxygen.

REACTIONS INVOLVED IN THE BIOLEACHING OF MINERAL SULFIDES

Bacterial leaching of  sulfide minerals relays on the combined use of two oxidants, ferric iron and oxygen. The semireaction associated to oxygen reduction is:

O2 + 4H+ + 4e    2H2O								         (1.8)

The E0 for this semi-reaction is + 1.229 V and the Nernst expression for its potential is:

EO2H2O=+1.229+RT4FlnpO2cH+4					                 (1.9)

With this high standard potential oxygen is thermodynamically adequate to oxidize ferrous iron. However, the rate of ferrous iron oxidation in abiotic conditions is too slow to be considered as a attractive technological alternative.  On the other hand, the oxidation of ferrous iron with oxygen is strongly catalyzed in the presence of leaching microorganisms. In 1970 it was reported that Acidithiobacillus ferrooxidans increased the rate of ferrous iron oxidation by a million times compared with the abiotic chemical oxidation of ferrous iron with dissolved oxygen.  There is a variety of microorganisms which catalyze ferrous iron oxidation and/or catalyze the oxidation  of reduced sulfur compounds. Table 1 give a list of the most commonly found microorganisms and their main characteristics.

Given the strong catalytic influence of leaching microrganisms on ferrous iron oxidation, leaching of a mineral sulfide can be conducted according to the reaction scheme shown in Figure 2. Electrons released by the mineral sulfide are accepted by ferric iron which results in the dissolution of the sulfide and the formation of ferrous iron. Simultaneously, with the help of bacteria ferrous iron is continuously transfering electrons to the dissolved  oxygen, which regenerates ferric iron and produces water, according to the global reaction:

1/2O2 + 2Fe+2 + 2H+    2Fe+3 + H2O						      (1.10)

Ferric iron acts as an intermediate oxidant which is continuously consumed and generated. Oxygen does not directly attack the sulfide but provides a steady thermodynamic driving force for the sulfide dissolution and acts as the final acceptor of the electrons released from

|  |  |  | Substrate for growing |  |  |  |  | Carbon source |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
| Microorganisms | Temp. [ºC] | pH | Fe+2 | S0 | FeS2 | CuFeS2 | S406 | CO2 | Yeast extract |
| Acidithiobacillus ferrooxidans | 10-30 | 1.4-3.5 | + | + | + | + | + | + | - |
| Thiobacillus thiooxidans | 10-40 | 1.3-4.5 | - | + | -/+ | -/+ | + | + | - |
| Leptospirilum ferrooxidans | 10-35 | 1.3-3.5 | + | - | + | -/+ | - | + | - |
| S. thermosulfoxidans | 40-50 |  | + | + | + | + | - | + | + |
| Sulfolobus BC | 70-90 | 1.6-2.5 | + | + | + | + | + | + | + |

Table 1. - Characteristics of main leaching microorganisms.

Fe+3 + e-  Fe+2

O2 + 4H+ + 4e-   2H2O

Cu+2 + S0  + 2e  CuS

+ 1.229

+ 0.77

+ 0.55

e-

e-

Figura 2.1. - Flow of electrons between semi-reactions involved in bioleaching of covellite

bacteria

the sulfide.  The global  reaction for the case of covellite leaching is obtained adding reactions 5 and 11,  which gives:

1/2O2 + CuS + 2H+   Cu+2 + S0 + H2O					     	      (1.11)

A similar reaction can be obtained for the case of chalcopyrite leaching:

O2 + CuFeS2 + 4H+  Cu+2 + Fe+2 + 2S0 + 2 H2O				                  (1.12)

Therefore, oxygen is the only oxidant consumed in the leaching process, and this is obtained from air which  is supplied by natural or forced aireation. There is also net consumption of acid which is related to the acid required  for ferrous iron oxidation (reaction 11). In industrial processes there is additional acid consumption linked to the neutralization of species present in the gangue.

In industrial processes acid is supplied as sulfuric acid.  However, the acid required can be partially generated by the following processes which occur during bioleaching:

a) Oxidation of residual elemental sulfur subproduct obtained from the ferric leaching of sulfides. Oxydation of elemental sulfur with oxygen occurs under the catalytic action of bacteria attached to the mineral surface, and can be represented  according to the reaction:

S0 + 3/2O2 + H2O  H2SO4							       (1.13)

As usually residual sulfur forms a barrier fro the diffusion of reactives and products through the  sulfide/solution iterface, this bacterial action can also have a catalytic influence on the copper dissolution rate.

b) Ferric leaching of pyrite, a mineral sulfide which is normally present  in copper sulfide ores and concentrates. In this case the sulfide contained in the mineral is directly oxidized to sulfate and the mineral dissolves according to the reaction:

14Fe+3 + FeS2 + 8H2O  15Fe+2 + 16H+ + 2SO4=					      (1.14)

c) Ferric iron precipitation. Ferric iron concentration normally increases in leaching solutions as a result of the partial dissolution of ferrous iron contained in sulfide minerals or gangue material, followed by bacteerial oxidation. A fraction of this ferric iron precipitates as jarosites, reaction which releases a fraction of the acid consumed in the ferric iorn formation. The generic reaction for jarosites formation is :

X+ + 3Fe+3 + 2SO4= + 6H2O  XFe3(SO4)2(OH)6 + 6H+ 				       (1.15)

where X+ corresponds to a monovalent cation,  either: Na+ (sodium jarosite), K+ (potassium jarosites), NH4+ (ammonium jarosites), H3O+ (hydronium jarosite) or Ag+ (silver jarosite).

KINETICS AND MICROBIOLOGICAL CONTROL IN BIOLEACHING

The economic succes of a bioleaching operation is very dependent on the rate of dissolution of copper from the sulfides present. Faster copper leaching rates are desirable as they imply smaller residence times and heaps or reactors of smaller size. The rate of sulfides dissolution in bioleaching is the result of a close interaction between  microbiological and metallurgical phenomena. This sections intend to describe the nature of some of these phenomena,  focusing at this stage on the interdependence of the kinetics of bio-oxidation of ferrous iron and ferric leaching of copper sulfides.  Understanding this aspect will provide an initial  conceptual base to understand the factors with determine copper leaching rate at different stages during a bioleaching process.

The reaction scheme in Figure 3 show that sulfide dissolution involves a chain to transfer electrons from to dissolved oxygen, the final electron acceptor.  In some situations the rate of electron transfer in this chain can be controlled by the rate of ferrous iron oxidation, which provides the oxidant for the sulfide dissolution. In other situations the rate of electron transfer can be controlled by the kinetics of ferric leaching of the sulfide.  The predominance of one or other type of control depends on the charateristics of the  kinetic of each reaction and the solution conditions.  The following two sections.  some basis aspects of the kinetics of ferric leaching of copper sulfides and ferrous iron oxidation. In the last section that conceptual base  is used to chacterize the different types of control and applied to analize the evolution of condictions in an experiment of copper concentrate bioleaching in a stirred bioreactor.

Fe+3

Fe+2

H+, O2

H2O

CuxS

e-

O2 (air)

(Solution)

Figure 3. - Electron transport in the bioleaching of sulfides in the presence of Fe+2, Fe+3 ions

T.f.

Cu+2

KINETICS OF MINERAL SULFIDE DISSOLUTION

Dissolution of a mineral sulfide involves two semireactions each of one having specific kinetic behaviour. The kinetics of each of each of these semireactions can be determined in electrochemical experiments in a three electrode cell in which the working electrode is made of a crystal of copper sulfide mineral (see Figure 4.1). During leaching of a sulfide particle with ferric ion the anodic dissolution of the sulfide is localized on certain zones which act as anodes, and Fe+3 reduction is localized on other zones which act as cathodes. This schematically represented in Figure 4.2a for the case of chalcopyrite dissolution.  The  i-E curve characteristic of the kinetics of chalcopyrite anodic dissolution can be obtained in an iron-free acid solution, by sweeping the potential of the sulfide towards  potentials anodic to the sulfide rest potential (see curve a in Figure 4.2b). The i-E curve characteristic of the kinetics of ferric ion reduction  can be obtained in an acid solution containing ferric ion, by cycling the potential towards cathodic potentials (see curve b in Figure 4.2b).

If the sulfide particle is immersed in a ferric iron – free solution the established potential ECp corresponds to the sulfide equilibrium potential and there is not dissolution (ECp in Figure 4.2b). When ferric iron is present in the solution the potential established in the sulfide shifts to more anodic potentials reaching a steady-state value in which  the anodic and cathodic currents are equal (EDIS in Figure 4.2b). The anodic current density established at that potential, ia,  is directly related to the rate of sulfide dissolution and can be calculated from the expression:

vMS=ia4F										     (4.1)

where ia is in (A/cm2) and vMS in (moles of MS/MS surface x seg).

The rate of sulfide dissolution increases with an increase in the Fe+3/Fe+2 ratio in solution, which results in a shift of EDIS   towards more anodic values and and increase of ia.  With the increase of the leaching time the decrease of the diameter of the unreacted sulfide core and the formation of a subproduct layer of elemental sulfur  produces a decrease of the currents associated to the anodic an cathodic subprocesses. As a consequence, there is a continuous decay of the rate of sulfide dissolution, as it is graphically represented in Figure 4.3.

The dependence of the sulfide dissolution rate with the Fe+3/Fe+2 ratio and leaching time can be expressed in general terms by the following kinetic expression:

vMS=vMSmaxαMSMS1 + B[Fe2+][Fe3+] 								(4.2)

where vMS is  MS/seg.  MS is the specific surface of MS (cm2 MS/mol MS) and  MS is the concentration of MS (mol/l). The value of vMSmax  decreases with leaching giving account of the decay in the reversibility of the anodic and cathodic subprocesses.

Reference electrode,  Ag/AgCl

V

Potentiostat

1

2

3

Working electrode (mineral sulfide)

Reference electrode (Ag/AgCl)

Counterelectrode (platinum foil)

Figure 4.1. - Thre-electrode electrochemical cell for characterization of anodic and cathodic subprocesses in minerals sulfide leaching.

Fe

+3

Fe

+2

Fe

+2

Cu

+2

S

o

I

e

-

i  (mA/cm

2

)

I

1

CuFeS

2



Cu

2+

+ Fe

2+

+ S

0

+ 4e

-

Fe

+3

+  e

-



Fe

2+

(-)

(+)

I

1

E, V vs SHE

a

b

E

Fe+3/Fe+2

E

Cp

i

c

e

-

Cu

+2

Fe

+2

S

0

i

a

CuFeS2 + 4Fe+3  Cu+2 + 5Fe+2 + 2S0

Fe

+3

Fe

+2

e

4.2a

4.2b

Figure 4.2. - Relation between sulfide leaching rate and the anodic and  cathodic subprocesses.

Fe

+3

Fe

+2

Fe

+2

Cu

+2

S

o

e

-

i  (mA/cm

2

)

I

1

Fe

+3

+  e

-



Fe

2+

(-)

(+)

I

2

I

3

t

1

t

2

t

3

t

1

t

2

t

3

E, V vs SHE

CuFeS

2



Cu

2+

+ Fe

2+

+ S

0

+ 4e

-

Fe

+3

Fe

+2

Cp

Fe

+2

Fe

+3

e

-

e

-

Cp

Cu

+2

Fe

+2

S

0

t3 > t2 > t1

Figure 4.3. - Influence of leaching time on the kinetics of the anodic and cathodic subprocesses and the sulfide leaching rate.

KINETICS OF BACTERIAL OXIDATION OF FERROUS IRON

Leaching bacteria uses the free energy released in the oxidation of ferrous iron with oxygen to activate its metabolism and grow. During bacterial respiration electrons are transferred from ferrous iron located in the periplasmic space to oxygen located in the inner side of the membrane (see Figure 5.1).  Bacteria grow by incorporating CO2 present in the air and continuously duplicate (see Figure 5.2). If N0 is the initial number of bacteria (per ml), the number of bacteria  (per ml) after one generation will be:

N1 = 2N0  										(5.1)

after two generations.

N2 = 2x2N0 										(5.2)

and after n  generations.

Nn = 2n N0										(5.3)

Taking logarithm in both sides:

nlnN=nln2+lnN0								(5.4)

Then if in a period t = t the bacterial population increases from N0 to N  bact/ml, the number of generations can be calculated according to the equation:

n=lnN−lnN0ln2								(5.5)

The average duplication time is calculated as:

τ=tn										(5.6)

then the number of generations is:

n=tτ										(5.7)

Figure 5.1. - Scheme of the pattern of charge transfer accross theperiplasmic space and  membrane of Acidithiobacillus ferrooxidans

Fe+3/Fe+2

CO2

e-

O2/H2O

nutrients

1st generation            2nd generation         3rd generation

Figure 5.2. - Bacterial grow from the free energy obtained from ferrous iron oxidation and subsequents  incorporation of CO2  from air.

Replacing  n in equation 5.4 the population of bacteria at time t = t  is:

lnN=lnN0+tτln2								(5.8)

Deriving and rearranging:

dlnNdt=ln2τ									(5.9)

1NdNdt=ln2τ									(5.10)

The term on the left corresponds to the specific growth rate of the microorganism, which is defind as .   Integrating, the number of bacteria at any time is given by the expression:

N=N0e−μt									(5.11)

which shows that the bacterial population grows exponentially.

Bacterial population expressed as N, bacteria/ml, is related to bacterial mass according to the expression:

X=NVρ										(5.12)

where X is the mass of bacteria (gr/ml), V is the volume of each bacteria and  is the bacteria density (gr/ml). The mass concentration of bacteria at any time is then given by:

X=X0e−μt									(5.13)

Bacterial yield, Y, is defined as  the ratio between the bacterial mass grown and the substrate mass consumed. In the case of bacteria grown out of the oxidation of ferrous iron the yield referred to the consumed ferrous iron is:

Y=−dXdtdFe+2dt								(5.14)

Then:

dFe+2dt=−1YdXdt								(5.15)

and the rate of ferrous iron oxidation can be expressed in terms of  as:

dFe+2dt=vFe+2=−μYX							(5.16)

The specific rate of bacterial growth, , is related to the concentration of ferrous iron in solution  through the Monod type equation:

μ=μmaxFe+2Km+Fe+2								(5.17)

The parameter max represents the máximum specific growth rate and Ks is the concentration of ferrous iron in which  = 1/2max (see Figure 5.3)

Finally, the rate of bacterial ferrous iron oxidation  can be expressed in the following kinetic expression:

vFe+2=−1Y∗μmax[Fe+2]XKm+[Fe+2]						(5.18)

if max/Y = vmax, the expression becomes:

vFe+2=−vmax[Fe+2]XKm+[Fe+2]							(5.19)



max

max

Km

Fe+2

Figure 5.3. - Dependence of the specific growth rate with ferrous iron concentration

In the case of Acidithiobacillus ferrooxidans the influence of ferric iron on the kinetics of ferrous iron has been recognized and been introduced in the form of an inhibition product (competitive inhibition) (ref):

vFe2+=vmax[Fe2+]X[Fe2+]+Km1+KI[Fe3+]  					(5.20)

which can be simplified to :

vFe2+=vMaxX1+K∗[Fe3+][Fe2+]								(5.21)

BACTERIAL AND CHEMICAL CONTROL IN BIOLEACHING

The  kinetic expressions for the ferric leaching of a mineral sulfide and the bacterial oxidation of ferrous iron depend on the Fe+3/Fe+2 ratio, in other words, the solution Eh. The rate of  ferric leaching of the sulfidecan be directly compared to the rate of bacterial oxidation of ferrous iron if ,  instead of expressing it as vMS, mol MS dissolved/seg, is expressed in terms of   v+Fe+2 , mol of Fe+2 generated/seg. For instance, in the case of ferric leaching of covellite (see equation   )  of   v+Fe+2 = 2vMS.

Figure 6.1 represents the rate of ferrous iron consumption, related to bacterial oxidation, ferrous iron formation, related to ferric leaching of the sulfide, as a function of solution Eh. There are differents curves for ferrous iron oxidation kinetics which corresponds to different bacterial populations, being X1 > X2 >X3 > X4  . There are also represented different curves for ferrous iron generated by ferric leaching which corresponds to the decay of sulfide reactivity during leaching time.  For a given population of bacteria and a given leaching time, characterized for a specific value of vMSmax , the leaching solution reaches a pseudo steady-state Eh where the rate of generation and consumption of ferrous are equal. This corresponds in each situation to the points where  the respective curves intersect with each other.

In certain operating conditions the Eh established in the leaching solution can be very low, being most of the dissolved iron as ferrous iron. This is usually the case at the start of bioleaching process when the fresh mineral sulfide, with high reactivity, is contacted with a leaching solution normally containing a small bacterial population. This situation corresponds to the case of curve of vFe+2   with X4  and curve of v+Fe+2 with vMSmax1 , which cross with each other at Eh approximately 0.52 V(SHE) (see pint A in Figure 6).  It is important to outline that in this situation most of the dissolved iron would be present in the leaching solution  as ferrous iron, but this should not be interpreted as an unefficient situation. In fact in these conditions a reactor can show high bacterial activity and high rates of sulfide leaching.  It is important to mention,  however,  that in these operating conditions the rate of sulfide dissolution can be enhanced by activating bacterial activity or increasing bacterial population.

Another extreme situation is reached when the mineral sulfide, with low reactivity after a certain leaching time, is in contact with a leaching solution containing a high population of leaching microorganisms.  This situation corresponds to the case of curve  vFe+2   with X1  and curve  v+Fe+2 with vMSmax4, , which cross with each other at Eh approximately 0.88 V(SHE) (see point B in Figure 6.1).  In this situation  the rate of sulfide dissolution is controlled by the intrinsic kinetics of  sulfide dissolution, which is normally controlled by diffusion phenomena occurring through the layer of solid subproducts and precipitates formed on  the sulfide surface.  Activating the bacterial dissolution of the reduced sulfur compounds present in this layer can in some cases help to increase the rate of sulfide dissolution.

In bioleaching reactors the operating conditions vary between the two extremes cases shown above.  A good demostrative case is presented in Figure 6.2 which shows the evolution of Eh, pH, copper concentration, iron concentration and bacterial population

0.50.550.60.650.70.750.80.850.9

Solution Eh, V(SHE)

vFe+2

v+Fe+2

X1

X2

X3

X4

Figure 6.1. - Rate of bacterial ferrous iron oxidation and chemical ferrous iron generation as a function of Eh.

A

B

during bioleaching of a copper concentrate in a batch stirred lab-scale bioreactor. In the industrial bioleaching of sulfide concentrates in tanks in series, the Eh in the leaching solution should increase from the initial units to tha final ones as the ratio X/vFe+2max increases with the residence time of the pulp in the process.  In heap leaching operations low Eh should be found in those solutions which are irrigating the sections which contain fresh ore.