## Slide 1
GEOTECHNICAL ENGINEERING IN RESIDUAL SOILS University of Chile, Santiago PART 5 : GEOTECHNIAL PROPERTIES OF RESIDUAL SOILS

## Slide 2: Measurement and Determination of Properties
Normal tube sampling for laboratory tests can be difficult in some types of material (presence of partly weathered material etc)
- alternatives are
in situ testing
block sampling
back analysis

## Slide 3: Block sampling – advantages
1) Can be obtained with minimal disturbance
2) Can be much larger than tube samples
3) Location can be selected after careful visual inspection – right material is sampled
Block sampling – disadvantages
Can only be obtained at or near the surface
Not so easy to handle and store as tubes.

## Slide 4: Block sampling: - note that plastic sheeting for wrapping sample immediately after trimming is essential

## Slide 5
Dr Morgenstern and his students taking a block sample

## Slide 6: Influence of sample disturbance

## Slide 7: Note (from previous figure) that disturbance can affect measurements of both peak strength, and stiffness

## Slide 8: Notes on in situ (field) testing – especially cone penetrometer tests
Presence of relic rock may prevent penetration
Assumption of undrained behaviour may not be valid
Dense highly weathered materials may give low values because particles are crushed
“Pumice” sand with very soft grains shows almost no variation in cone resistance with density.
Stress history and OCR are normally irrelevant
Above factors mean interpretation of test results requires caution.

## Slide 9: Difficulty of laboratory or field measurement of soil properties can sometimes be overcome by back analysis procedures:
Records of foundation settlement can be analysed to obtain compressibility/stiffness parameters
Slope failures can be analysed to obtain shear strength parameters
Even intact slopes can be used to obtain strength parameters (with limitations)

## Slide 10: Sample preparation before laboratory testing:
Drying soil before measurement of particle size, Atterberg limits, compaction properties, or even Specific Gravity can change the results with some soils – especially volcanic soils.
Good practice is not to dry the soil any more than necessary to carry out the test. For example if the test is the Plastic Limit, the soil should be dried only to the Plastic limit.

## Slide 11: Particle Size Measurements:
With most residual soils, particle size measurements can be made in the usual manner. Two exceptions:
Soils containing a large proportion of highly weathered particles – particles get broken up. (Accurate measurement not so important)
Clays of high allophane content flocculate during sedimentation (hydrometer) tests. Hard to overcome but particle size not very important.
Are particle size measurements much use? Yes – but not as useful as Atterberg Limits.

## Slide 12: Atterberg Limits
For fine grained soils these are much more useful than particle size measurements
We still need to recognise that to carry out the tests the soil must be remoulded
Some soils become progressively more plastic the greater the remoulding

## Slide 13: Usefulness of Atterberg Limits
Position of the soil on the Plasticity Chart
Relationship of natural water content to the Liquid and Plastic limit

## Slide 14: Plasticity Chart - Position in Relation to the A-line

## Slide 15
Rice fields in Bali, Indonesia – volcanic ash soil
Soil: very high LL, well below the A-line.(allophane)

## Slide 16
Slip failure on very gentle slope, Java, Indonesia
Soil: “Black cotton” clay from sedimentary rocks - old shales. High LL, well above A-line (montmorillinite)

## Slide 17: The clay from previous slide

## Slide 18: “Reference Density States, Density Indicies” and Porosity LI for clay Rd for sand

## Slide 19: Properties of Undisturbed Samples:
Permeability:
Generalisations are risky, but it is certainly true that water flows/seeps much more quickly through residual soils than sedimentary soils
This is partly because of the presence of discontinuities, and partly because of the higher permeability of intact material
Remoulding generally substantially reduces the coefficient of permeability

## Slide 20: Compressibility, as Measured in the Oedometer Test.
Despite its “defects” it is still the most common method of measuring soil compressibility for estimating foundation settlement

## Slide 21: Oedometer tests on three undisturbed red clay samples
Log graphs suggest a preconsolidation pressure
Linear graphs show a different story

## Slide 22: Oedometer tests on volcanic ash samples – conventional log graphs
These graphs suggest clear pre-consolidation pressures, at least with some of the samples.

## Slide 23: The same oedometer tests – using a linear scale
This graph shows true behaviour
– some samples show a pre-consolidation pressure
– others do not

## Slide 24: Another example of log and linear plots
Linear plot shows no trace of a pre-consolidation pressure

## Slide 25: Residual soils may or may not show a pre-consolidation pressure
Only the use of a linear plot will establish the existence of a pre-consolidation pressure
This “pre-consolidation” results from the weathering process – it is not related to stress history
This “pre-consolidation” stress is better called a vertical “yield” stress.
The need to use linear plots has been stressed by various authors - Janbu (1979), Wesley (1983), Vaughan (1985) and Verdugo (1992).

## Slide 26: Three types of compression behaviour from oedometer tests

## Slide 27: Selection of stiffness parameters from oedometer tests for settlement estimates - mv or cc/cs ?
Plot the results using both log and linear scales for pressure
Determine the stress range over which compression of the soil will take place
Use this information judge the more appropriate parameters to use

## Slide 28: Field evidence of yield stress

## Slide 29: mv for some residual soils

## Slide 30: Time Rate of Settlement, As Indicated by Oedometer Tests

## Slide 31: Some typical root time graphs from residual soils - where is the straight line section?

## Slide 32: Influence of Remoulding on Consolidation Rate

## Slide 33: There is an upper limit to the value of the coefficient of consolidation that can be measured in a conventional oedometer test
The highest value is about 0.1 m2/day (=0.012 cm2/sec)
Soils with cv values higher than this will not show straight lines on normal root time graphs
If reliable cv values are required then a pore pressure dissipation test in a triaxial cell would be necessary

## Slide 34: A theoretical, or conceptual, framework for understanding deformation behaviour of residual soils
Firstly, what is our conceptual framework(s) for understanding the behaviour of sedimentary soils?

## Slide 35: This is a widely used “simplistic” framework that relates behaviour to initial void ratio and stress history from Vaughan (1985)

## Slide 36: Limitations of this framework:
OK for clays, but with sands the void ratio is not related just to stress history
For sands, the initial void ratio is a governing factor on the position and shape of the e-log graph
For sands, the e-log curves occupy different positions on the graph, and do not converge towards a common straight line, at least not over the stress range of interest to engineers.

## Slide 37: A second, related, “conceptual framework” is also used for both sands and clays
This framework involves identifying “density indicies” – these are a measure of the denseness of packing of the particles.
The actual density is related to reference “density states”.
The Liquidity Index and the Relative Density (or Density Index) are used for clay and sand respectively.

## Slide 38: Density Indicies for clay and sand

## Slide 39: Vaughan (1985) makes the following points:
Neither Relative Density nor LI are ideal for residual soils
Residual soils are not clean granular soils appropriate for relative density measurements
Residual soils often contain significant quantities of coarse material so Atterberg Limits are of limited use.
The concept of a density index involving reference “density states” is relevant to all soils.
Therefore it would be useful to develop such reference “density states” for residual soils.

## Slide 40: Vaughan suggests:
The maximum dry density from a standard Proctor compaction test would be a suitable substitute for the Plastic Limit.
To replace the Liquid Limit, a simple test to determine the water content at an undrained shear strength of 2 kPa could be devised.
Note that 2 kPa is considered to be the average undrained shear strength of clay at the Liquid Limit.

## Slide 41: Vaughan (contd.) suggests:
a new “density state” parameter embracing both Liquidity Index and Relative Density.
Defined as:
eR = 0 signifies a dense (low porosity)
state
eR = 1 signifies a low density (highly
porous) state.

## Slide 42: Density state and compressibility (Vaughan examples)
& (c) have e > eL and show a yield stress followed by high compressibility (highly structured soils)
(b) & (d) have e < eL and do not show a yield stress and are of low compressibility (not highly structured soils)

## Slide 43: Influence of remoulding is often valuable as an additional guide to soil characteristics.
The following examples illustrate density states & influence of remoulding on some residual soils
Note that these are fine grained soils so the reference states are simply Plastic and Liquid Limits.

## Slide 44: Red clay very dense, no structure no yield stress no effect from re-moulding

## Slide 45: Red clay – linear scale

## Slide 46: Volcanic ash (allophane)
a very porous material
strong structure
probably sensitive
probably showing a yield stress

## Slide 47: Volcanic ash - linear scale

## Slide 48: Silt (Weathered sandstone)
highly sensitive
strong structure influence

## Slide 49: Shear Strength of Residual Soils
- Undrained Strength

## Slide 50: Skempton’s (1957) relationship for sedimentary soils. Such correlations have little relevance to residual soils.

## Slide 51: Undrained shear strength versus Liquidity Index
Note: rapid decrease in Su with L.I. for remoulded soils little change in Su with L.I. For undisturbed soils.

## Slide 52: Effective strength parameters
Clay minerals present usually have good
frictional properties
Micro-structure often contributes
positively to shear strength – gives the
soil a significant c value
Macro-structure can be a very negative
influence that controls behaviour.

## Slide 53: Triaxial tests on a material containing discontinuities

## Slide 54: Triaxial test results on an intact material

## Slide 55: Examples of Behaviour in Triaxial Tests
Stress/strain curves, pore pressure behaviour and stress paths

## Slide 56: Consolidated undrained tests on a tropical red clay

## Slide 57: Tropical red clay – Cons Und. Triaxial tests – stress paths

## Slide 58: Consolidated undrained tests on a silt (from weathered sandstone)

## Slide 59: Silt – Cons Und. Triaxial tests – stress paths Note the “subtle” difference in behaviour between the undisturbed and remoulded soil

## Slide 60: Friction angle related to A-line

## Slide 61: Residual strength vs PI – not a good correlation

## Slide 62: Residual strength related to the A-line – a better correlation

## Slide 63: Some compaction characteristics of residual soils
Highly variable – no constant value of optimum water content
With some soils, natural water content may be well above optimum water content
Highly structured soils may steadily soften as compaction proceeds, and become progressively difficult to compact
Some soils, especially volcanic ash with high allophane content may have “flat” compaction curves, with no clear optimum water content

## Slide 64: Standard compaction test results from two small sites

## Slide 65: Compaction test from volcanic ash (allophane) clay

## Slide 66
FIN
GRACIAS POR SU ATENCION