Particle Size Conversion

Sieve Designation; Nominal Sieve Opening. Standard; Mesh; inches; mm; Microns. 25.4 mm; 1 in.; 1.00; 25.4; 25400. 22.6 mm; 7/8 in.; 0.875; 22.6; 22600. 19.0 mm; 3/4 in.; 0.750; 19.0; 19000. 16.0 mm; 5/8 in.; 0.625; 16.0; 16000. 13.5 mm; 0.530 in.; 0.530; 13.5; 13500. 12.7 mm; 1/2 in.; 0.500; 12.7; 12700. 11.2 mm; 7/16 in.; 0.438; 11.2; 11200. 9.51 mm; 3/8 in.; 0.375; 9.51; 9510. 8.00 mm; 5/16 in.; 0.312; 8.00; 8000. 6.73 mm; 0.265 in.; 0.265; 6.73; 6730. 6.35 mm; 1/4 in.; 0.250; 6.35; 6350. 5.66mm; No.3 1/2; 0.223; 5.66; 5660. 4.76 mm; No. 4; 0.187; 4.76; 4760. 4.00 mm; No. 5; 0.157; 4.00; 4000. 3.36 mm; No. 6; 0.132; 3.36; 3360. 2.83 mm; No. 7; 0.111; 2.83; 2830. 2.38 mm; No. 8; 0.0937; 2.38; 2380. 2.00 mm; No. 10; 0.0787; 2.00; 2000. 1.68 mm; No. 12; 0.0661; 1.68; 1680. 1.41 mm; No. 14; 0.0555; 1.41; 1410. 1.19 mm; No. 16; 0.0469; 1.19; 1190. 1.00 mm; No. 18; 0.0394; 1.00; 1000. 841 m; No. 20; 0.0331; 0.841; 841. 707 m; No. 25; 0.0278; 0.707; 707. 595 m; No. 30; 0.0234; 0.595; 595. 500 m; No. 35; 0.0197; 0.500; 500. 420 m; No. 40; 0.0165; 0.420; 420. 354 m; No. 45; 0.0139; 0.354; 354. 297 m; No. 50; 0.0117; 0.297; 297. 250 m; No. 60; 0.0098; 0.250; 250. 210 m; No. 70; 0.0083; 0.210; 210. 177 m; No. 80; 0.0070; 0.177; 177. 149 m; No. 100; 0.0059; 0.149; 149. 125 m; No. 120; 0.0049; 0.125; 125. 105 m; No. 140; 0.0041; 0.105; 105. 88 m; No. 170; 0.0035; 0.088; 88. 74 m; No. 200; 0.0029; 0.074; 74. 63 m; No. 230; 0.0025; 0.063; 63. 53 m; No. 270; 0.0021; 0.053; 53. 44 m; No. 325; 0.0017; 0.044; 44. 37 m; No. 400; 0.0015; 0.037; 37. Larger sieve openings (1 in. to 1/4 in.) have been designated by a sieve "mesh" size that corresponds to the size of the opening in inches. Smaller sieve "mesh" sizes of 3 1/2 to 400 are designated by the number of openings per linear inch in the sieve. The following convention is used to characterize particle size by mesh designation: - a "+" before the sieve mesh indicates the particles are retained by the sieve; - a "-" before the sieve mesh indicates the particles pass through the sieve; - typically 90% or more of the particles will lie within the indicated range. For example, if the particle size of a material is described as -4 +40 mesh, then 90% or more of the material will pass through a 4-mesh sieve (particles smaller than 4.76 mm) and be retained by a 40-mesh sieve (particles larger than 0.420 mm). If a material is described as -40 mesh, then 90% or more of the material will pass through a 40-mesh sieve (particles smaller than 0.420 mm). This information is also provided on page T848 of the Aldrich 2003-2004 Catalog/Handbook of Fine Chemicals..