## Slide 1
Activity 1 : Introduction to CCDs.
In this activity the basic principles of
CCD Imaging is explained.
Simon Tulloch smt@ing.iac.es

## Slide 2
What is a CCD ?
Charge Coupled Devices (CCDs) were invented in the 1970s and originally found application as
memory devices. Their light sensitive properties were quickly exploited for imaging applications
and they produced a major revolution in Astronomy. They improved the light gathering power of
telescopes by almost two orders of magnitude. Nowadays an amateur astronomer with a CCD camera
and a 15 cm telescope can collect as much light as an astronomer of the 1960s equipped with a
photographic plate and a 1m telescope.
CCDs work by converting light into a pattern of electronic charge in a silicon chip. This pattern of
charge is converted into a video waveform, digitised and stored as an image file on a computer.

## Slide 3
Photoelectric Effect.
The effect is fundamental to the operation of a CCD. Atoms in a silicon crystal have electrons arranged in
discrete energy bands. The lower energy band is called the Valence Band, the upper band is the Conduction
Band. Most of the electrons occupy the Valence band but can be excited into the conduction band by heating
or by the absorption of a photon. The energy required for this transition is 1.26 electron volts. Once in this
conduction band the electron is free to move about in the lattice of the silicon crystal. It leaves behind a ‘hole’
in the valence band which acts like a positively charged carrier. In the absence of an external electric field
the hole and electron will quickly re-combine and be lost. In a CCD an electric field is introduced to sweep
these charge carriers apart and prevent recombination.
Increasing energy
Valence Band
Conduction Band
1.26eV
Thermally generated electrons are indistinguishable from photo-generated electrons . They constitute a
noise source known as ‘Dark Current’ and it is important that CCDs are kept cold to reduce their number.
1.26eV corresponds to the energy of light with a wavelength of 1m. Beyond this wavelength silicon becomes
transparent and CCDs constructed from silicon become insensitive.
photon
photon
Hole Electron

## Slide 4
CCD Analogy
A common analogy for the operation of a CCD is as follows:
An number of buckets (Pixels) are distributed across a field (Focal Plane of a telescope)
in a square array. The buckets are placed on top of a series of parallel conveyor belts and collect rain fall
(Photons) across the field. The conveyor belts are initially stationary, while the rain slowly fills the
buckets (During the course of the exposure). Once the rain stops (The camera shutter closes) the
conveyor belts start turning and transfer the buckets of rain , one by one , to a measuring cylinder
(Electronic Amplifier) at the corner of the field (at the corner of the CCD)
The animation in the following slides demonstrates how the conveyor belts work.

## Slide 5
RAIN (PHOTONS)
BUCKETS (PIXELS)
VERTICAL
CONVEYOR
BELTS
(CCD COLUMNS)
HORIZONTAL
CONVEYOR BELT
(SERIAL REGISTER)
MEASURING
CYLINDER
(OUTPUT
AMPLIFIER)
CCD Analogy

## Slide 6
Exposure finished, buckets now contain samples of rain.

## Slide 7
Conveyor belt starts turning and transfers buckets. Rain collected on the vertical conveyor
is tipped into buckets on the horizontal conveyor.

## Slide 8
Vertical conveyor stops. Horizontal conveyor starts up and tips each bucket in turn into
the measuring cylinder .

## Slide 9
`
After each bucket has been measured, the measuring cylinder
is emptied , ready for the next bucket load.

## Slide 16
A new set of empty buckets is set up on the horizontal conveyor and the process
is repeated.

## Slide 33
Eventually all the buckets have been measured, the CCD has been read out.

## Slide 34
Structure of a CCD 1.
The image area of the CCD is positioned at the focal plane of the telescope. An image then builds up that
consists of a pattern of electric charge. At the end of the exposure this pattern is then transferred, pixel at a
time, by way of the serial register to the on-chip amplifier. Electrical connections are made to the outside
world via a series of bond pads and thin gold wires positioned around the chip periphery.
Connection pins
Gold bond wires
Bond pads
Silicon chip
Metal,ceramic or plastic package
Image area
Serial register
On-chip amplifier

## Slide 35
Structure of a CCD 2.
CCDs are are manufactured on silicon wafers using the same photo-lithographic techniques used
to manufacture computer chips. Scientific CCDs are very big ,only a few can be fitted onto a wafer.
This is one reason that they are so costly.
The photo below shows a silicon wafer with three large CCDs and assorted smaller devices. A CCD has
been produced by Philips that fills an entire 6 inch wafer! It is the worlds largest integrated circuit.
Don Groom LBNL

## Slide 36
Structure of a CCD 3.
One pixel
Channel stops to define the columns of the image
Transparent
horizontal electrodes
to define the pixels
vertically. Also
used to transfer the
charge during readout
Plan View
Cross section
The diagram shows a small section (a few pixels) of the image area of a CCD. This pattern is reapeated.
Electrode
Insulating oxide
n-type silicon
p-type silicon
Every third electrode is connected together. Bus wires running down the edge of the chip make the
connection. The channel stops are formed from high concentrations of Boron in the silicon.

## Slide 37
Structure of a CCD 4.
On-chip amplifier
at end of the serial
register
Cross section of
serial register
Image Area
Serial Register
Once again every third electrode is in the serial register connected together.
Below the image area (the area containing the horizontal electrodes) is the ‘Serial register’ . This also
consists of a group of small surface electrodes. There are three electrodes for every column of the image area

## Slide 38
Structure of a CCD 5.
The serial register is bent double to move the output amplifier away from the edge
of the chip. This useful if the CCD is to be used as part of a mosaic.The arrows
indicate how charge is transferred through the device.
Edge of
Silicon
160m
Image Area
Serial Register
Read Out Amplifier
Bus wires
Photomicrograph of a corner of an EEV CCD.

## Slide 39
Structure of a CCD 6.
OD
OS
RD
R
SW
Output
Node
Substrate
Output
Transistor
Reset
Transistor
Summing
Well
20m
Output Drain (OD)
Output Source (OS)
Gate of Output Transistor
Output Node
R
Reset Drain (RD)
Summing Well (SW)
Last few electrodes in Serial Register
Serial Register Electrodes
Photomicrograph of the on-chip amplifier of a Tektronix CCD and its circuit diagram.

## Slide 40
Electric Field in a CCD 1.
The n-type layer contains an excess of electrons that diffuse into the p-layer. The p-layer contains an
excess of holes that diffuse into the n-layer. This structure is identical to that of a diode junction.
The diffusion creates a charge imbalance and induces an internal electric field. The electric potential
reaches a maximum just inside the n-layer, and it is here that any photo-generated electrons will collect.
All science CCDs have this junction structure, known as a ‘Buried Channel’. It has the advantage of
keeping the photo-electrons confined away from the surface of the CCD where they could become trapped.
It also reduces the amount of thermally generated noise (dark current).
n
p
Electric potential
Potential along this line shown
in graph above.
Electric potential
Cross section through the thickness of the CCD

## Slide 41
Electric Field in a CCD 2.
During integration of the image, one of the electrodes in each pixel is held at a positive potential. This
further increases the potential in the silicon below that electrode and it is here that the photoelectrons are
accumulated. The neighboring electrodes, with their lower potentials, act as potential barriers that define
the vertical boundaries of the pixel. The horizontal boundaries are defined by the channel stops.
n
p
Electric potential
Region of maximum
potential

## Slide 42
pixel
boundary
Charge packet
p-type silicon
n-type silicon
SiO2 Insulating layer
Electrode Structure
pixel
boundary
incoming
photons
Charge Collection in a CCD.
Photons entering the CCD create electron-hole pairs. The electrons are then attracted towards
the most positive potential in the device where they create ‘charge packets’. Each packet
corresponds to one pixel

## Slide 43
Charge Transfer in a CCD 1.
In the following few slides, the implementation of the ‘conveyor belts’ as actual electronic
structures is explained.
The charge is moved along these conveyor belts by modulating the voltages on the electrodes
positioned on the surface of the CCD. In the following illustrations, electrodes colour coded red
are held at a positive potential, those coloured black are held at a negative potential.
1
2
3

## Slide 44
1
2
3
+5V
0V
-5V
+5V
0V
-5V
+5V
0V
-5V
Time-slice shown in diagram
1
2
3
Charge Transfer in a CCD 2.

## Slide 45
1
2
3
+5V
0V
-5V
+5V
0V
-5V
+5V
0V
-5V
1
2
3
Charge Transfer in a CCD 3.

## Slide 46
1
2
3
+5V
0V
-5V
+5V
0V
-5V
+5V
0V
-5V
1
2
3
Charge Transfer in a CCD 4.

## Slide 47
1
2
3
+5V
0V
-5V
+5V
0V
-5V
+5V
0V
-5V
1
2
3
Charge Transfer in a CCD 5.

## Slide 48
1
2
3
+5V
0V
-5V
+5V
0V
-5V
+5V
0V
-5V
1
2
3
Charge Transfer in a CCD 6.

## Slide 49
1
2
3
+5V
0V
-5V
+5V
0V
-5V
+5V
0V
-5V
1
2
3
Charge Transfer in a CCD 7.
Charge packet from subsequent pixel enters
from left as first pixel exits to the right.

## Slide 50
1
2
3
+5V
0V
-5V
+5V
0V
-5V
+5V
0V
-5V
1
2
3
Charge Transfer in a CCD 8.

## Slide 51
On-Chip Amplifier 1.
OD
OS
RD
R
SW
Output
Node
Output
Transistor
Reset
Transistor
Summing
Well
+5V
0V
-5V
+10V
0V
R
SW
--end of serial register
Vout
Vout
The on-chip amplifier measures each charge packet as it pops out the end of the serial register.
The measurement process begins with a reset
of the ‘reset node’. This removes the charge
remaining from the previous pixel. The reset
node is in fact a tiny capacitance (< 0.1pF)
RD and OD are held at
constant voltages
(The graphs above show the signal waveforms)

## Slide 52
On-Chip Amplifier 2.
OD
OS
RD
R
SW
Output
Node
Output
Transistor
Reset
Transistor
Summing
Well
+5V
0V
-5V
+10V
0V
R
SW
--end of serial register
Vout
Vout
The charge is then transferred onto the Summing Well. Vout is now at the ‘Reference level’
There is now a wait of up to a few tens of
microseconds while external circuitry measures
this ‘reference’ level.

## Slide 53
On-Chip Amplifier 3.
OD
OS
RD
R
SW
Output
Node
Output
Transistor
Reset
Transistor
Summing
Well
+5V
0V
-5V
+10V
0V
R
SW
--end of serial register
Vout
Vout
This action is known as the ‘charge dump’
The voltage step in Vout is as much as
several V for each electron contained
in the charge packet.
The charge is then transferred onto the output node. Vout now steps down to the ‘Signal level’

## Slide 54
On-Chip Amplifier 4.
OD
OS
RD
R
SW
Output
Node
Output
Transistor
Reset
Transistor
Summing
Well
+5V
0V
-5V
+10V
0V
R
SW
--end of serial register
Vout
Vout
Vout is now sampled by external circuitry for up to a few tens of microseconds.
The sample level - reference level will be
proportional to the size of the input charge
packet.