## Slide 1: Engineering Materials ІІ
TTT-diagrams

## Slide 2: Iron-carbon phase diagram

## Slide 3: TIME-TEMPERATURE-TRANSFORMATION CURVES

## Slide 4: THE BAINITE transformation

## Slide 5: The bainite transformation

## Slide 6: TTT-diagram OF AN EUTECTOID STEEL

## Slide 7: Diffusionless transformation

## Slide 8: Martensite

## Slide 9: martensite

## Slide 10: Retained Austenite
A large volume expansion when martensite forms from austenite.
As the martensite plates form during quenching, they surround and isolate small pools of austenite.
for the remaining pools of austenite to transform, the surrounding martensite must deform.
Because the strong martensite resists the transformation, either the existing martensite cracks or the austenite remains trapped in the structure as retained austenite.
Notes: Listón“: lath

## Slide 11: Hypo and hypereutectoid steels

## Slide 12: Hypo and hypereutectoid steels

## Slide 13: Isothermal heat treatment

## Slide 16: martempering

## Slide 17: austempering

## Slide 19: Continuous cooling transformations (CCT)

## Slide 20: Continuous cooling transformations (CCT)

## Slide 21: Continuous cooling transformations (CCT)

## Slide 22: Continuous cooling transformations (CCT)